## Slide 1: Packaging

## Slide 2: Packaging Requirements
Desired package properties
Electrical: Low parasitics
Mechanical: Reliable and robust
Thermal: Efficient heat removal
Economical: Cheap
Wire bonding
    Only periphery of chip available for IO connections
    Mechanical bonding of one pin at a time (sequential)
    Cooling from back of chip
    High inductance (~1nH)
http://www.embeddedlinks.com/chipdir/package.htm
More about packaging:

## Slide 3: Chip to package connection
Flip-chip
    Whole chip area available for IO connections
    Automatic alignment
    One step process (parallel)
    Cooling via balls (front) and back if required
    Thermal matching between chip and substrate required
    Low inductance (~0.1nH)

## Slide 4: Bonding Techniques

## Slide 5: Tape-Automated Bonding (TAB)

## Slide 6: New package types
BGA (Ball Grid Array)
    Small solder balls to connect to board
    small
    High pin count
    Cheap
    Low inductance
CSP (Chip scale Packaging)
    Similar to BGA
    Very small packages
Package inductance:
1 - 5 nH

## Slide 7: Flip-Chip Bonding

## Slide 8: Package-to-Board Interconnect

## Slide 9: Package Types
Through-hole vs. surface mount
From Adnan Aziz http://www.ece.utexas.edu/~adnan/vlsi-05/

## Slide 10: Chip-to-Package Bonding
Traditionally, chip is surrounded by pad frame
  Metal pads on 100 – 200 mm pitch
  Gold bond wires attach pads to package
  Lead frame distributes signals in package
  Metal heat spreader helps with cooling
From Adnan Aziz http://www.ece.utexas.edu/~adnan/vlsi-05/

## Slide 11: Advanced Packages
Bond wires contribute parasitic inductance
Fancy packages have many signal, power layers
  Like tiny printed circuit boards
Flip-chip places connections across surface of die rather than around periphery
  Top level metal pads covered with solder balls
  Chip flips upside down
  Carefully aligned to package (done blind!)
  Heated to melt balls
  Also called C4 (Controlled Collapse Chip Connection)
From Adnan Aziz http://www.ece.utexas.edu/~adnan/vlsi-05/

## Slide 12: Package Parasitics
Use many VDD, GND in parallel
  Inductance, IDD
From Adnan Aziz http://www.ece.utexas.edu/~adnan/vlsi-05/

## Slide 13: Signal Interface
Transfer of IC signals to PCB
  Package inductance.
  PCB wire capacitance.
  L - C resonator circuit generating oscillations.
  Transmission line effects may generate reflections
  Cross-talk via mutual inductance
L
C
Package
Chip
PCB trace
L-C Oscillation
Z
Transmission line reflections
R
f =1/(2p(LC)1/2)
L = 10 nH
C = 10 pF
f = ~500MHz

## Slide 14: Package Parameters

## Slide 15: Package Parameters

## Slide 16: Package Parameters
2000 Summary of Intel’s Package I/O Lead Electrical Parasitics for Multilayer Packages

## Slide 17: Packaging Faults
Small Ball Chip Scale Packages (CSP) Open

## Slide 18
CSP Assembly on 6 mil Via in 12 mil pad
Void over via structure
Packaging Faults

## Slide 19: Miniaturisation of Electronic Systems
Enabling Technologies :
  SOC
  High Density Interconnection technologies
    SIP – “System-in-a-package”
From ECE 407/507 University of Arizona
http://www.ece.arizona.edu/mailman/listinfo/ece407

## Slide 20: The Interconnection gap
Improvement in density of standard interconnection and packaging technologies is much slower than the IC trends
IC scaling
Time
Size scaling
PCB scaling
Interconnect Gap
Advanced PCB
Laser via
From ECE 407/507 University of Arizona
http://www.ece.arizona.edu/mailman/listinfo/ece407

## Slide 21: The Interconnection gap
Requires new high density Interconnect technologies
IC scaling
Time
Size scaling
PCB scaling
Advanced PCB
Reduced Gap
Thin film lithography based
Interconnect technology
From ECE 407/507 University of Arizona
http://www.ece.arizona.edu/mailman/listinfo/ece407

## Slide 22: SoC has to overcome…
  Technical Challenges:
      Increased System Complexity.
      Integration of heterogeneous IC technologies.
      Lack of design and test methodologies.
  Business Challenges:
      Long Design and test cycles
      High risk investment
      Hence time to market.
  Solution
      System-in-a-Package
From ECE 407/507 University of Arizona
http://www.ece.arizona.edu/mailman/listinfo/ece407

## Slide 23: Multi-Chip Modules

## Slide 24: Multiple Chip Module (MCM)
Increase integration level of system (smaller size)
Decrease loading of external signals > higher performance
No packaging of individual chips
Problems with known good die:
  Single chip fault coverage: 95%
  MCM yield with 10 chips: (0.95)10 = 60%
Problems with cooling
Still expensive

## Slide 25: Complete PC in MCM